## Slide 1
Metal Sulfide Nanograins as Shell Wall on Wide Band Gap Metal Oxide Nanofiber Heterostructure: Efficient Visible Photocatalytic Activity through Bandgap Narrowing
Introduction
Designing Metal sulfide as a shell layer has interested the construction of new set of heterostructure which induces the narrow band function at the interlayers with attracted functional properties for promising remediation based applications. Construction of heterostructures on electrospun nanofiber initiates the directionated carrier mobility and effective charge separation with nanograin assembled structural morphology.
Shell wall thickness on narrowing the band gap
-- core shell interface from surface
Visible response
-- Visible active by bandgap narrowing
suppression of carrier recombination
-- Oxygen and sulfur induces defect
with type II band function
ZnS, CuS, Ag2S and Bi2S3 based shell layer on ZnO Nanofibers
First, through the sulfidation process ZnO-ZnS based heterostructure was constructed on electrospun ZnO nanofiber with different shell wall thickness.
Promising Metal sulfur interaction on surface
Variable oxygen related defects
Change in valance band position
Visible response by narrow bandgap shell functionality
Secondly, addition metal impurities were added in the sulfidation process to construct the ZnO-CuS, ZnO-Ag2S, ZnO-Bi2S3 based core shell heterostructural nanofibers.
Narrow band function on wide band gap semiconductors
External sulfide based shell wall induced narrow band function on electrospun wide band semiconductors such as TiO2, ZnO, ZnTiO3, BaTiO3, SrTiO3 having a surface nanograined architecture resembling higher surface interaction.
MSx shell on MTiO3 (M= Zn, Sr and Ba) Nanofibers
To overcome the demerits of ZnO and TiO2, MTiO3 (M= Zn, Sr, Ba) nanofibers were prepared and sulfidated for constructing the MTiO3-MS core shell nanofibers, where S ions react with the M sites in the MTiO3 crystal structure.
Higher surface roughness lead to enhanced surface area and core-shell NFs exhibit higher visible response on compared to pristine NFs
Supports
References
CONCLUSION & FUTURE WORK
[1] F. Xiao, J. Miao et al., Small. 2015, 11, 2115-2130.
[2] Junyu Zhang et al., Mater. Chem. Front, 2017, 1, 231-250.
[3] Ranjith et al., Catalysis Science and Technology, 2017, 8, 1167- 1180.
[4] Sovio J. A. Monix et al., Energy and Environment Science, 2015, 8, 731-759.
[5] Yajun Wang et al., Nanoscale, 2013, 5, 8326-8339.
In sulfidation process, the stable TiO2 leads to monolayer decoration of TiS3 shell functionality with optical gain through the oxygen defects along with the sulfur interstitial defects.
Strongly red-shifted absorption with minimized valance band position
Visible emission induced through the sulfur induced defects
Inducing deeper perception and understanding of core-shell heterostructured NF architecture which play a critical role in improving visible catalytic activity by narrowing the band gap. It could initiate possible functional hybrid systems with metal sulfide counterparts for photoresponsive tunable functional applications.
Strong appearance of S2- state on the catalyst surface
Mono or thin layered TiS3 Shell on TiO2 nanofiber
Core-shell NF catalyst were visibly active with higher degrading rate with effective production of ROS
Visible catalytic behavior and byproduct quantifying
Through grained surface S ions migrated, which later induces the different shell wall thickness on nanofiber morphology.
M-S shell wall induces the change in band function for effective carrier separation in core shell NFs
Enhanced visible catalytic behavior
Effective carrier separation promotes the ROS
Higher photo corrosive stability
Stable catalytic properties even after 8 reusable cycle with structural stability
Selective sulfidation on titanate fibers leads to the homogeneous sulfide based heterostructures through the surface interaction.
f
1µm
1µm
1µm
500 nm
500 nm
500 nm
Calcined
at
400°C
0 min
Increasing the sulfidation time
Shell wall controlled MO/MS NFs
Polymer complex
(PVA)/PVP
Metal precursor
Polymer/Metal
precursor composites NFs
Metal oxide NFs
0 min
180 min
540 min
ZnO NFs
ZnS NFs
ZnO-ZnS core-shell NFs
S
Zn
O
1 μm
1 μm
100 nm
100 nm
2 nm
Ti
Zn
O
S
2 nm
Electrospun MTiO3 NF
Sulfidated MTiO3 -MS NF
CB
CB
VB
VB
2.54
to
3.04
2.42
2.20
0.89
E (eV)
E (eV)
-0.63
to
-0.20
CB
3.17 eV -3.4 eV
2.58 eV
2.28 eV
Pristine M-O NFs
Sulfur modified M-O NFs
CB: Conduction Band VB: Valance Band
500 nm
500 nm
500 nm
e-
h+
hv
O2
O2-
H2O
.OH
Pollutant molecules
CO2 + H2O
CB
VB
3.2 eV
2.28 eV
2.58 eV
Ov
SO3
VB
CB
Carbon impurities
Sulfur defect states
Oxygen vacancies of metalic states
e-
e-
e-
e-
h+
h+
h+
h+
3.2 eV
2.6 eV
3.2 eV
2.4 eV
Extended visible
absorption
Increased oxygen
Vacancies
Minor trace of S2-
on surface
Band gap narrowed due to strained conduction band minimum energies and improves the efficiency of interfacial charge separation.
314 eV
2.28 eV
ZnO
ZnO-Ag2S
ZnO-CuS
ZnO-Bi2S3
a
f
d
b
e
c
h
g
Ag2S
Bi2S3
CuS
ZnO
ZnO-ZnS
ZnS
100 nm
100 nm
100 nm
100 nm
10 nm
5 nm
5 nm
5 nm
0.26 nm
0.31 nm
0.24 nm
0.29 nm
TiO2
TiO2-TiS3
TiO2-TiS3:Na
ZnTiO3
ZnTiO3-ZnS
SrTiO3-SrS
300 nm
500 nm
BaTiO3-BaS
Ranjith Shanmugam, Anitha Senthamizhan, Brabu Balusamy and Tamer Uyar
UNAM--Institute of Materials Science and Nanotechnology, Bilkent University, Ankara, 06800-Turkey
tamer@unam.bilkent.edu.tr